EVERBUILD MAMMOTH ELECTRICAL INSULATION TAPE

| Colour | Product Code | Pack Size | Box Qty |
| --- | --- | --- | --- |
| Black | 2ELEC33BK | 19mm x 33Mtr | 48 |
| Blue | 2ELECBN | 19mm x 33Mtr | 48 |
| Green | 2ELECGRN | 19mm x 33Mtr | 48 |
| Red | 2ELECRED | 19mm x 33Mtr | 48 |
| White | 2ELECWE | 19mm x 33Mtr | 48 |
| Yellow/Green | 2ELECYELGRN | 19mm x 33Mtr | 48 |
| Yellow | 2ELECYW | 19mm x 33Mtr | 48 |
| Brown | 2ELECBN | 19mm x 33Mtr | 48 |
| 7 Mixed Colours | 2ELEC33MIX | 19mm x 33Mtr | 48 |

(The mixed box contains 12 black, and 6 of each of the other colours - excluding Brown)

Product Description

EVERBUILD Mammoth Electrical insulation tape is an easy to unwind PVC electrical tape for providing insulation for most electrical wires.

Benefits

- Available in a variety of colours.

- Flame retardant.

- Manufactured to BS EN60454 Type 2 and IEC454-2

Limitations

- Do not use on surfaces that bleed oils or plasticiser.

- Always check rating of cable to be insulated.

- It is the users responsibility to determine suitability for use. If in doubt contact technical services for advice.

Application

Ensure surfaces to which tape is to be applied are clean sound and dry. Remove outer packaging from roll of tape. Peel required amount of tape from roll pressing firmly into place while unrolling ensuring all bare wire is covered. Cut with a knife or tear off when finished.

Specific Data

| Type Of Film | PVC |
| --- | --- |
| Thickness | 0.13mm |
| Tensile Strength | 2.5 Kg/com |
| Elongation @ Break | 200% |
| Adhesion | 18 Kg/cm |
| Dielectric Strength | 1250 volts/mil |
| Dielectric Breakdown | 6500 volts |

Storage

Store in cool dry conditions between 5 and 250C. Safe in normal use however as a precaution keep polythene outer packaging away from children.

Shelf Life

36 months from date of manufacture.

The technical data contained herein is based on our present knowledge and experience and we cannot be held liable for any errors, inaccuracies, omissions or editorial failings that result from technological changes or research between the date of issue of this document and the date the product is acquired. Before using the product, the user should carry out any necessary tests in order to ensure that the product is suitable for the intended application. Moreover, all users should contact the seller or the manufacturer of the product for additional technical information concerning its use if they think that the information in their possession needs to be clarified in any way, whether for normal use or a specific application of our product. Our guarantee applies within the context of the statutory regulations and provisions in force, current professional standards and in accordance with the stipulations set out in our general sales conditions. The information detailed in the present technical data sheet is given by way of indication and is not exhaustive. The same applies to any information provided verbally by telephone to any prospective or existing customer.