CONSTRUCTION PRODUCTS REGULATION

DECLARATION OF PERFORMANCE

No:   HYBSMP/1-CPR/ 2014

Substrate:	Anodised aluminium and Mortar M1

Primer:		No primer on Aluminium, Sikaflex Primer 3-N for Mortar

| 1. Identification Code | Everbuild TECNIC HYRIFLEX SMP Codes: FPHYBSMP |
| --- | --- |
| 2. Type, Batch and/or Serial Number | - For batch number - see packaging |
| 3. Intended use | Sealant for non-structural use in joints in buildings and pedestrian walkways Part 1: Sealants for Façade elements |
| 4. Manufacturer | Everbuild Building Products ltd, Site 41, Cross Green Industrial Estate, Knowsthorpe Way, Leeds, LS9 0SW |
| 5. Authorised Representative | Not Applicable |
| 6. Assessment and Verification of Constancy of Performance | System 3 |
| 7. Notified Body and Tasks | SKZ Notified Body No. 1213 |
| 8. European Technical Assessment | Not Applicable |
| 9. Declared Performance TO EN15651-1 (2012) |  |
| Type | F EXT-INT-CC |
| Classification | F25HM |
| Reaction to Fire | Class E |
| Loss of Volume ISO10563 | ≤10% |
| Resistance to flow ISO7390 | ≤3 mm |
| Adhesion/cohesion properties at maintained extension after water immersion (23°C) ISO 10590 | NF |
| Adhesion/cohesion properties ISO 8340 modified (-30°C) | NF |
| Durability ISO 8340, ISO 9047 and ISO 10590 | Pass |

Substrate:	Anodised aluminium and Mortar M1

Primer:		No primer on Aluminium, Sikaflex Primer 3-N for Mortar

| 1. Identification Code | Everbuild TECNIC HYRIFLEX SMP Codes: FPHYBSMP |
| --- | --- |
| 2. Type, Batch and/or Serial Number | - For batch number - see packaging |
| 3. Intended use | Sealant for non-structural use in joints in buildings and pedestrian walkways Part 3: Sealants for Sanitary elements |
| 4. Manufacturer | Everbuild Building Products ltd, Site 41, Cross Green Industrial Estate, Knowsthorpe Way, Leeds, LS9 0SW |
| 5. Authorised Representative | Not Applicable |
| 6. Assessment and Verification of Constancy of Performance | System 3 |
| 7. Notified Body and Tasks | SKZ Notified Body No. 1213 |
| 8. European Technical Assessment | Not Applicable |
| 9. Declared Performance TO EN15651-4 (2012) |  |
| Type | PW EXT-INT-CC |
| Classification | PW25HM |
| Reaction to Fire | Class E |
| Loss of Volume ISO10563 | ≤10% |
| Resistance to flow ISO7390 | ≤3 mm |
| Adhesion/cohesion properties at maintained extension (23°C) ISO 8340 | NF |
| Tear Resistance ISO 8340 modified | NF |
| Adhesion / Cohesion properties at maintained extension 28 days water immersion (23°C) ISO 10590 modified | NF change of secant modulus: ≤50% |
| Adhesion / Cohesion properties at maintained extension 28 days salt water immersion (23°C) ) ISO 10590 modified | NF |
| Adhesion/cohesion properties at maintained extension (-30°C) ISO 8340 modified | NF |
| Durability ISO 8340, ISO 9047 and ISO 10590 | Pass |

The performance of the product identified in points 1 and 2 is in conformity with the declared performance in point 9 . The declaration of performance is issued under the sole responsibility of the manufacturer identified in point 4.

Signed:         I. G. Southerington – Head of Technical               P.R. Thomas – Technical Manager

Dated:  Leeds, 12/6/14